DuPont Performance Coatings

Color Formula Inquiry

| From | Michael Kalok (65Vettemike) | Date | 03.03.2004 |
| --- | --- | --- | --- |

| Formula Standard # | 680699 |  | Years Used | 1965 - 1966 |
| --- | --- | --- | --- | --- |
| EU Stock # / Alt # | 1 |  | Lead (Pb) Free | Y |
| Color Name | MAROON |  | PCP | N |
| Formula Owner Region | UNITED STATES |  | Quality | 600 - CENTARI 600 |
| Formulation Date | 29.04.1999 |  | Value Shade | 6 |
| Coat | BASECOAT (1) |  | Paint Code | 988 |
| EU Alt Color Change |  |  |  |  |
| Color Owner | GENERAL MOTORS CORP |  |  |  |

Ingredients

| Quantity To Mix | 1 LITER (100.0% Fill) |  | Ingredient Display Units | GRAMS |
| --- | --- | --- | --- | --- |

| Ingredient | Ingr Quality | Description | Amount | Accum. Amount |
| --- | --- | --- | --- | --- |
| AM85 |  | TRANSPARENT MAROON | 89,3 | 89,3 |
| AM86 |  | OPAQUE RED | 70,1 | 159,4 |
| AM55 |  | LIGHT RED | 20,1 | 179,5 |
| AM5 |  | JET BLACK | 11,7 | 191,2 |
| AM16 |  | MEDIUM FINE ALUMINIUM | 8,0 | 199,2 |
| AB150 |  | BINDER (LMC) | 367,0 | 566,2 |
| AB160 |  | BINDER (HMC) | 365,2 | 931,4 |